# Guide Schedule of Sampling and Testing for Design-Build Projects by the Independent Quality Firm (IQF)

## May 1, 2026

© 2026 by Texas Department of Transportation

All Rights Reserved

## Contents

Using the DB Guide Schedule	1

Embankments, Subgrades, Backfill, and Base Courses	4

Asphalt-Treated Base (Plant Mixed)	30

Seal Coat	36

Hydraulic Cement Concrete – Structural (Classes: C, F, H, S, CO, K, LMC, or SS)	42

Hydraulic Cement Concrete – Non-Structural Concrete (Classes: A, B, or E)	53

Grout (Various Applications)	55

Hydraulic Cement Concrete Pavement (Classes: P or HES)	58

Hot-Mix Asphalt Pavement (Items 341, 342, 344, 346, 347, and 348)	68

### Using the DB Guide Schedule

The Independent Quality Firm (IQF) will perform materials sampling at locations and timing defined in this Guide Schedule of Sampling and Testing for Design-Build Projects by the IQF (hereafter referred to as the DB Guide Schedule). This minimum testing frequency must be met with random independent or random split samples as defined in the Quality Assurance Program for CDA / Design-Build Projects (DB QAP), Section 3.3, “Sampling and Testing.” During the startup of new categories of work and when there are any concerns regarding the quality of materials, the IQF will conduct sampling and testing at a higher frequency.

The IQF will determine random sample locations using American Society for Testing and Materials (ASTM) D3665. While the testing of random independent or random split samples is required to meet the requirements of this DB Guide Schedule, the IQF will perform additional (fixed) tests when the quality of material is questionable at a location other than the randomly selected location. These fixed tests will constitute an acceptance test, and a failing result must be addressed in a similar manner to a failing random test. Fixed tests will not count toward meeting minimum IQF testing frequencies. The IQF will meet this DB Guide Schedule sampling and testing frequency for all materials (permanent and temporary) for each Specification item, grade, supplier, material, and test method combination established by TxDOT in its sole discretion. TxDOT will establish these combinations in a manner to differentiate materials that are required to meet various Specifications, produced and/or stored in separate physical locations, or as otherwise determined by TxDOT, in its sole discretion, for appropriate material acceptance purposes.

Research of sampling and testing rates listed for project tests in this DB Guide Schedule show that the risk of either rejecting “good” material or accepting “bad” material ranges from 20% to 40%. To reduce this risk, the sampling rate will be increased during initial production. A four-fold increase in testing frequency will generally reduce risk to approximately 5%. The intent of increasing testing at the start of production is to ensure that the DB Contractor’s processes are in control and to establish acceptability requirements early.

The IQF can use results from TxDOT’s Material Producer List (MPL). For materials listed on the MPL, the IQF will be required to perform job control tests as defined by the TxDOT DB Guide Schedule. Materials that are not monitored or not preapproved by TxDOT under the MPL are subject to IQF and Owner Verification Firm (OVF) sampling and testing as part of the acceptance program, except as noted in the remarks of this document. Materials not listed on the MPL require the Materials and Tests Division’s (MTD’s) testing and approval before these materials are used on the project. Non-preapproved materials must be sampled and tested in accordance with the applicable Departmental Material Specifications (DMSs), applicable material quality program, and Specifications. The IQF will audit and verify that materials delivered to the project site are in conformance with approved materials submittals. The IQF and TxDOT’s designee will use approved laboratories from the MPL when applicable. Testing to be performed by MTD as noted in this document will be at the DB Contractor’s expense. Testing charges will be based on rates in effect at the time MTD testing services are performed. TxDOT’s Inspection and Testing Rates are published at Inspection & Testing Rates.

When using materials or processes that are listed on the TxDOT MPL, the DB Contractor will furnish additional samples of materials to be incorporated into the work at TxDOT’s request. Manufacturer’s warranties, guarantees, instruction sheets, parts lists, and other materials that are furnished with articles or materials incorporated into the work will be made available to TxDOT upon request.

Other testing required by the Specifications but not shown in the DB Guide Schedule should be performed at a frequency required by the applicable DMS and applicable material quality program, and as necessary to provide adequate confidence that materials meet Specifications.

Note: The referee laboratory will be TxDOT MTD’s central laboratory or MTD’s designated independent third-party testing laboratory qualified in accordance with the DB QAP, Section 4, and approved in advance by MTD to serve as the referee laboratory for the project.

### Embankments, Subgrades, Backfill, and Base Courses

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

Table 1 - Embankments, Subgrades, Backfill, and Base Courses.

| Material or Product | Test For | Test Number | Project Tests: Location or Time of Sampling | Project Tests: Frequency of Sampling4 | Remarks |
| --- | --- | --- | --- | --- | --- |
| Embankments (Cuts & Fills) | Liquid Limit1 | Tex-104-E | During stockpiling operations, from completed stockpile, or project site2 | Materials with Plasticity Index (PI) ≤15: 10,000 cubic yards (CY) | For Type A embankment or when required by the plans. Determine a new liquid limit and plasticity index for each different material or notable change in material. Sample in accordance with Tex-100-E. |
| Embankments (Cuts & Fills) | Plasticity Index1 | Tex-106-E | During stockpiling operations, from completed stockpile, or project site2 | Materials with PI >15: 5,000 CY | For Type A embankment or when required by the plans. Determine a new liquid limit and plasticity index for each different material or notable change in material. Sample in accordance with Tex-100-E. |
| Embankments (Cuts & Fills) | Gradation | Tex-110-E, Part 1 | During stockpiling operations, from completed stockpile, or project site2 | Each 10,000 CY | When shown on plans. Sample in accordance with Tex-100-E. |
| Embankments (Cuts & Fills) | Moisture/ Density | Tex-114-E | During stockpiling operations, from completed stockpile, or project site2 | As directed by the IQF | Not required for ordinary compaction. Ordinary compaction shall not be used on main lanes. Determine a new optimum moisture and maximum density for each different material or notable change in material. Sample in accordance with Tex-100-E. |
| Embankments (Cuts & Fills) | In-Place Density1 | Tex-115-E, Part 1 | As designated by the IQF | Fill: each 5,000 CY Minimum 1 per lift Cut: each 6,000 linear feet (LF) | Not required for ordinary compaction. Ordinary compaction shall not be used on main lanes. Determine a new optimum moisture and maximum density according to Tex-114-E for each different material or notable change in material. Correct the moisture contents measured by nuclear density gauge in Tex-115-E with the moisture contents determined in accordance with Tex-103-E, as necessary for control, for each different material or notable change in material, and adjust the density accordingly. |
| Embankments (Cuts & Fills) | Moisture Content (Roadway) 1 | Tex-115-E, Part 1 | As designated by the IQF | Fill: each 5,000 CY Min 1 per lift Cut: each 6,000 LF | Not required for ordinary compaction. Ordinary compaction shall not be used on main lanes. Correct the moisture contents measured by nuclear density gauge in Tex-115-E with the moisture contents determined in accordance with Tex-103-E, as necessary for control, for each different material or notable change in material, and adjust the density accordingly. |
| Retaining Wall (Non-Select Backfill) | As shown above for Embankment (Cuts & Fills) | As shown above for Embankment (Cuts & Fills) | As shown above for Embankment (Cuts & Fills) | As shown above for Embankment (Cuts & Fills) | Sample in accordance with Tex-100-E. |
| Retaining Wall (Select Backfill) | Plasticity Index1 | Tex-106-E | During stockpiling operations, from completed stockpile, or project site2 | Each 5,000 CY | Required only for Type CS backfill. Sample in accordance with Tex-100-E. |
| Retaining Wall (Select Backfill) | Gradation | Tex-110-E, Part 1 | During stockpiling operations, from completed stockpile, or project site2 | Each 5,000 CY | Required only for drainage aggregate. Sample in accordance with Tex-100-E. |
| Retaining Wall (Select Backfill) | Gradation | Tex-401-A | During stockpiling operations, from completed stockpile, or project site2 | Each 5,000 CY | Required for select backfill. Sample in accordance with Tex-100-E. |
| Retaining Wall (Select Backfill) | Resistivity1 | Tex-129-E | During stockpiling operations, from completed stockpile, or project site2 | Each 5,000 CY | For material with resistivity between 1,500 ohm-centimeter (ohm-cm) and 3,000 ohm-cm, determine chloride and sulfate content, as specified in Item 423. Sample in accordance with Tex-100-E. |
| Retaining Wall (Select Backfill) | pH1 | Tex-128-E | During stockpiling operations, from completed stockpile, or project site2 | Each 5,000 CY | Sample in accordance with Tex-100-E. |
| Retaining Wall (Select Backfill) | Magnesium Soundness | Tex-411-A | During stockpiling operations, or from completed stockpile | 1 per source | Test when backfill sources appear to contain particles such as shale; caliche; or other soft, poor-durability particles. Micro-Deval test may be used instead of the soundness test when the Micro-Deval test results are not >20%. Sample in accordance with Tex-100-E and submit to MTD for testing before use. |
| Retaining Wall (Select Backfill) | Micro-Deval Abrasion | Tex-461-A | During stockpiling operations, or from completed stockpile | 1 per source | Micro-Deval test results may be used instead of soundness when test results are not >20%. When percent loss from Micro-Deval test is >20%, the magnesium soundness test governs aggregate verification. Sample in accordance with Tex-100-E. |
| Retaining Wall (Select Backfill) | In-Place Density1 | Tex-115-E, Part 1 | As designated by the IQF | 1 per backfill lift, per wall | Not required for rock backfill. For walls greater than 500 feet (ft.) in length, perform 1 test per lift for every 500 ft. in length.4 Correct the moisture contents measured by nuclear density gauge in Tex-115-E with the moisture contents determined in accordance with Tex-103-E for each different material or notable change in material, and adjust the density accordingly. |
| Untreated Subgrade | Uniformity: Dynamic Cone Penetration (DCP) 1 | ASTM D6951 | As designated by the IQF | 1 per 250-LF section (when using proof rolling) 1 per 250-LF or 1,000-LF section (when using intelligent compaction (IC) data) 4 | When using proof rolling: Perform 1 test for every 250-LF section after proof rolling is complete in accordance with Item 216 and after unstable and rutted (>0.5 inch [in.]) areas are corrected. When using proof mapping IC data: Perform 1 test for every 250-LF section of roadbed for those locations classified as “red-mapped,” or as directed by the IQF. Perform 1 test for every 1,000-LF section of roadbed for non-“red-mapped” locations. Perform testing on the final subgrade layer after curing per Specification requirements. |
| Untreated Base Courses | Liquid Limit1 | Tex-104-E | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Sample in accordance with Tex-100-E. Not required for crushed concrete unless otherwise shown on the plans. |
| Untreated Base Courses | Plasticity Index1 | Tex-106-E | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Sample in accordance with Tex-100-E. Not required for crushed concrete unless otherwise shown on the plans. |
| Untreated Base Courses | Crushed Face Count1 | Tex-460-A, Part 1 | During stockpiling operations, or from completed stockpile | Each 20,000 CY | Required for Type C crushed gravel only. |
| Untreated Base Courses | Gradation1 | Tex-110-E, Part 1 | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Sample in accordance with Tex-100-E. |
| Untreated Base Courses | Percent Passing #200 Sieve | Tex-111-E | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | The #200 sieve test is only required to meet the waiver of the unconfined compressive strength requirement and is only applicable to stockpile samples from Section 247.2.4., “Stockpile Approval.” Waived when flex base is mixed with or without existing material and treated with cement, emulsion, foamed asphalt, or lime, unless otherwise shown on the plans. Sample in accordance with Tex-100-E. |
| Untreated Base Courses | Deleterious Material1 | Tex-413-A | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Required for Type (Ty) D material, which includes Ty A material or crushed concrete. Sample in accordance with Tex-100-E. |
| Untreated Base Courses | Sulfate Content1 | Tex-145-E, Part 2 | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Required for Ty D material which includes Ty A material or crushed concrete. Sample in accordance with Tex-100-E. |
| Untreated Base Courses | Moisture/ Density | Tex-113-E | From completed stockpile at the source3 | Each 20,000 CY | Ordinary compaction is not allowed. Sample in accordance with Tex-100-E. |
| Untreated Base Courses | Wet Ball Mill1 | Tex-116-E, Parts 1 and 2 | From completed stockpile at the source3 | Each 20,000 CY | Required for Grades 1–2 and Grade 5, and as shown on the plans for Grade 4. Not required for crushed concrete unless otherwise shown on the plans. Sample in accordance with Tex-100-E. |
| Untreated Base Courses | Strength | Tex-117-E, Part 2 | From completed stockpile at the source3 | Each 20,000 CY | Required for Grade 1–Grade 2 and Grade 5, and as shown on the plans for Grade 4. When base material is from a source where the District has a record of satisfactory triaxial results, the frequency of testing may be reduced to 1 per 30,000 CY. If any 1 test falls below the minimum value required, the frequency of testing will return to the original frequency of 20,000 CY. Unconfined compressive strength testing may be waived when meeting the #200 sieve requirement for Grade 1–2 only, unless otherwise shown on the plans. Sample in accordance with Tex-100-E. |
| Untreated Base Courses | In-Place Density | Tex-115-E, Part 1 | As designated by the IQF | Each 3,000 CY Min 1 per lift4 | Ordinary compaction is not allowed. Correct the moisture contents measured by nuclear density gauge in Tex-115-E with the moisture contents determined in accordance with Tex-103-E, as necessary for control, for each different material or notable change in material, and adjust the density accordingly. |
| Untreated Base Courses | Moisture Content (Roadway) 1 | Tex-115-E, Part 1 | As designated by the IQF | Each 3,000 CY Min 1 per lift4 | Ordinary compaction is not allowed. Correct the moisture contents measured by nuclear density gauge in Tex-115-E with the moisture contents determined in accordance with Tex-103-E, as necessary for control, for each different material or notable change in material, and adjust the density accordingly. |
| Untreated Base Courses | Thickness1 | Tex-140-E | As designated by the IQF | Each 3,000 CY Min 1 per lift4 | None |
| Untreated Base Courses | Ride Quality1 | Tex-1001-S, Surface Test Type B | Final riding surface of all travel lanes | Each travel lane | Only applies to the final travel lanes that receive a 1- or 2-course surface treatment for the final surface, unless otherwise shown on the plans. |
| Treated Subgrade and Base Courses – Subgrade Before Treatment | Organic Content | Tex-148-E | As designated by the IQF | Min 1 per source, or more frequently as needed | Required for existing subgrade material and material imported from a borrow source. Soil survey and geologic maps may be used to determine sampling locations. Higher testing frequency shall be performed when changes in the material are observed. When treating with lime and results fail to meet Specification, the IQF may perform a pH series or as directed. This will determine whether there is a significant decrease in pH to justify using more lime. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – Subgrade Before Treatment | Sulfate Content | Tex-145-E, Part 2 | As designated by the IQF | 1 per 500-LF section or 5,000 CY | Required for existing subgrade material and material imported from a borrow source. Soil survey and geologic maps may be used to determine sampling locations. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Liquid Limit1 | Tex-104-E | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | When central mix site or plant is used, windrow sampling may be waived. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Plasticity Index1 | Tex-106-E | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Gradation1 | Tex-110-E, Part 1 | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Percent Passing #200 Sieve | Tex-111-E | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | The #200 sieve test is only required to meet the waiver of the unconfined compressive strength requirement and is only applicable to stockpile samples from Section 247.2.4., “Stockpile Approval.” Waived when flex base is mixed with or without existing material and treated with cement, emulsion, foamed asphalt, or lime, unless otherwise shown on the plans. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Deleterious Material1 | Tex-413-A | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Required for Ty D material, which includes Ty A material or crushed concrete. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Sulfate Content1 | Tex-145-E, Part 2 | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Required for Ty D material, which includes Ty A material or crushed concrete. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Crushed Face Count1 | Tex-460-A, Part 1 | During stockpiling operations, or from completed stockpile | Each 20,000 CY | Required for Type C crushed gravel only. |
| Treated Subgrade and Base Courses – New Base Material | Wet Ball Mill1 | Tex-116-E, Parts 1 and 2 | From completed stockpile at the source3 | Each 20,000 CY | Required for Grade 1–Grade 2 and Grade 5, and as shown on the plans for Grade 4. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – New Base Material | Strength1 | Tex-117-E | From completed stockpile at the source3 | Each 20,000 CY | The compressive strength of the flexible base is waived unless otherwise shown on the plans. When required for Grade 1–Grade 2 and Grade 5, and as shown on the plans for Grade 4. When base material is from a source where the District has a record of satisfactory triaxial results, the frequency of testing may be reduced to 1 per 30,000 CY. If any 1 test falls below the minimum value required, the frequency of testing will return to the original frequency of 20,000 CY. |
| Treated Subgrade and Base Courses – Lime | Compliance with DMS-6350 | Tex-600-J | During delivery to project | Commercial lime slurry, quicklime dry and slurry: Each 200 ton of lime, per source | Sample in accordance with Tex-600-J. Verify the source is listed on the current MPL for commercial lime slurry. Only materials appearing on the MPL will be accepted. Verify the sources for quicklime are listed on the MPL. If not on the MPL, sample the material at a rate of 1 per source and submit to MTD for testing before use. |
| Treated Subgrade and Base Courses – Cement | Compliance with DMS-4600 | N/A | Railroad car, truck, or cement bins | N/A | Verify the source is listed on the current MPL for cement. If not, sample in accordance with DMS-4600 and submit to MTD for testing before use. |
| Treated Subgrade and Base Courses – Uncompacted Mixtures | Pulverization Gradation | Tex-101-E, Part 3 | Roadway, after pulverization and mixing | As necessary for control | At the beginning of the project, 1 test must be made for each 4,500 CY or 6,000 tons until the IQF is satisfied that acceptable pulverization results are being obtained. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – Uncompacted Mixtures | Moisture/ Density Curve | Part 1 for Tex-120-E, Tex-121-E, Tex-122-E, or Tex-134-E | From roadway after treatment | As necessary for control | Ordinary compaction is not allowed. Perform a new moisture/density curve for each different or notable change in material and at the direction of the IQF. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – Uncompacted Mixtures | Strength | Part 2 for Tex-120-E, Tex-121-E, Tex-122-E, or Tex-134-E | From roadway after treatment | Each 20,000 CY (or higher frequency as directed by TxDOT—see remarks) | For cement-treated base (CTB): A higher sampling and testing frequency of 1 test per day of production will be at TxDOT’s sole discretion for CTB layers that are part of the pavement section. Sample in accordance with Tex-100-E. |
| Treated Subgrade and Base Courses – Compacted Mixtures | In-Place Density1 | Tex-115-E, Part 1 | As designated by the IQF | Each 3,000 CY Min 1 per lift4 | Ordinary compaction is not allowed. Determine the appropriate moisture/density curve for each different material or notable change in material. Correct the moisture contents measured by nuclear density gauge in Tex-115-E with the moisture contents determined in accordance with Tex-103-E, as necessary for control, for each different material or notable change in material, and adjust the density accordingly. Stabilizers and materials such as Reclaimed Asphalt Pavement (RAP), gypsum, and iron ore tend to bias the counts for nuclear density gauges. |
| Treated Subgrade and Base Courses – Compacted Mixtures | Moisture Content (Roadway) 1 | Tex-115-E, Part 1 | As designated by the IQF | Each 3,000 CY Min 1 per lift4 | Ordinary compaction is not allowed. Correct the moisture contents measured by nuclear density gauge in Tex-115-E with the moisture contents determined in accordance with Tex-103-E, as necessary for control, for each different material or notable change in material, and adjust the density accordingly. |
| Treated Subgrade and Base Courses – Compacted Mixtures | Thickness1 | Tex-140-E | As designated by the IQF | Each 3,000 CY Min 1 per lift4 | None |
| Treated Subgrade and Base Courses – Compacted Mixtures | Uniformity: DCP (Treated Subgrade Layer Only) 1 | ASTM D6951 | As designated by the IQF | 1 per 250-LF section (when using proof rolling) 1 per 250 LF or 1,000-LF section (when using IC equipment) 4 | When using proof rolling: Perform 1 test for every 250-LF section after proof rolling is complete in accordance with Item 216 and unstable and rutted (>0.5 in.) areas are corrected. When using proof mapping IC data: Perform 1 test for every 250-LF section of roadbed for those locations classified as “red-mapped,” or as directed by the IQF. Red-mapped areas are locations not achieving at least 25% of the intelligent compaction measured value (ICMV). Perform 1 test for every 1,000-LF section of roadbed for non-“red-mapped” locations. Perform testing on the final treated subgrade layer after curing per Specification requirements. |
| Untreated Base Courses –RAP and Other Recycled Materials | Sulfate Content1 | Tex-145-E, Part 3 | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Required only for DB-Contractor furnished recycled material. Not required for RAP. Sample in accordance with Tex-100-E. |
| Untreated Base Courses –RAP and Other Recycled Materials | Deleterious Material1 | Tex-413-A | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Required only for DB-Contractor furnished recycled material. Sample in accordance with Tex-100-E. |
| Untreated Base Courses –RAP and Other Recycled Materials | Decantation | Tex-406-A, Part 1 | During stockpiling operations, from completed stockpile, or windrow2 | Each 5,000 CY | Required only for DB-Contractor furnished RAP. Sample in accordance with Tex-100-E. |

1. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log or Non-Conformance Report Log.

2. The IQF will select any of these locations or any combinations thereof with the provision that the initial sample will be obtained from the completed stockpile at the source, and the following samples will be taken at the project site (from the windrow for treated and untreated bases and embankments).

3. The IQF will sample from the completed stockpile at the source and test before placement.

4. Each test performed that is based on a quantity of material (or section length) is considered “or fraction thereof” for calculating number of tests.

### Asphalt-Treated Base (Plant Mixed)

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

Table 1A – Asphalt-Treated Base (Plant Mixed).

| Material or Product | Test For | Test Number | Project Tests: Location or Time of Sampling | Project Tests: Frequency of Sampling6 | Remarks |
| --- | --- | --- | --- | --- | --- |
| Aggregate | Liquid Limit5 | Tex-104-E | During stockpiling operations, from completed stockpile, or before mixing | Each 5,000 CY | Sample in accordance with Tex-100-E. |
| Aggregate | Plasticity Index5 | Tex-106-E | During stockpiling operations, from completed stockpile, or before mixing | Each 5,000 CY | Sample in accordance with Tex-100-E. |
| Aggregate | Wet Ball Mill5 | Tex-116-E, Parts 1 and 2 | During stockpiling operations, from completed stockpile, or before mixing | 1 per source | Sample in accordance with Tex-100-E. |
| RAP and Recycled Aggregate | Decantation | Tex-406-A, Part 1 | During stockpiling operations, from completed stockpile, or before mixing | Each 10,000 CY | Sample in accordance with Tex-100-E. |
| Lime | Compliance with DMS-6350 | Tex-600-J | During delivery to the project | Commercial lime slurry, quicklime dry and slurry: Each 200 ton of lime per source6 | Sample in accordance with Tex-600-J and submit to MTD for testing before use. On projects requiring <50 tons per source, material from MTD-approved sources may be accepted on the basis of producer’s certification without sampling. Verify the sources for commercial lime and quick lime are listed on the MPL. If not on the MPL, sample the material at a rate of 1 per source and submit to MTD for testing before use. |
| Asphalt Binder | Compliance with Item 300 | N/A | Sampling port nearest to the storage tank. Take project samples when designated by the IQF. | 1 per grade, per source | Test a minimum of 1 sample taken from the project. Sample binder in accordance with Tex-500-C. Verify that the binder is from a preapproved source when it arrives at the project, and that the lab number on the shipping ticket is within the valid dates shown in the MTD Quality Monitoring (QM) test report. |
| Tack Coat | Compliance with Item 300 | N/A | Distributor | 1 per grade, per source | Test a minimum of 1 sample taken from the project. Sample tack coat in accordance with Tex-500-C. Verify that the binder is from a preapproved source when it arrives at the project, and that the lab number on the shipping ticket is within the valid dates shown in the MTD QM test report. |
| Mix Design Verification | Compliance with applicable Specification | Tex-204-F, Part 4 | At source (if not approved) | Min 1 design per mix type and asphalt grade | Verify that aggregates, recycled asphalt pavement, mineral filler, asphalt binder, anti-stripping additives, and warm mix systems are on the MPL, where applicable, and that they meet project Specification requirements. Project sampling and testing may be conducted on individual materials as necessary for control. |
| Complete Mixture | Lab-Molded Density5 | Tex-207-F, Part 1 | Truck sample | 20,000 CY (25,000 tons) | Sample in accordance with Tex-222-F. |
| Complete Mixture | Gradation5 | Tex-200-F, Part 1 | Truck sample | 20,000 CY (25,000 tons) | Sample in accordance with Tex-222-F. Determine the gradation of the aggregate from the complete mixture tested in accordance with Tex-236-F. |
| Complete Mixture | Percent Asphalt5 | Tex-236-F | Truck sample | Each 1,500 CY (2,000 tons) or days production | Determine correction factors for ignition oven using Tex-236-F once every 12 months (mo.) or more frequently as needed. Sample in accordance with Tex-222-F. |
| Complete Mixture | Indirect Tensile Strength – Dry5 | Tex-226-F | Truck sample | 1 per mix design | Sample in accordance with Tex-222-F. |
| Complete Mixture | Moisture Content5 | Tex-212-F, Part 2 | Truck sample | 1 per mix design | Sample in accordance with Tex-222-F. |
| Complete Mixture | Moisture Susceptibility | Tex-530-C | As designated by the IQF | 1 per mix design | Sample in accordance with Tex-222-F. |
| Roadway | In-Place Air Voids5 | Tex-207-F, Part 1 or 6/ Tex-227-F, Part 1 or 2 or 3 | Roadway cores, as designated by the IQF6 | Each 3,000 CY Min 1 per lift | Ordinary compaction is not allowed. Sample in accordance with Tex-222-F. |
| Roadway | Ride Quality5 | Tex-1001-S surface test Type A | On finished surface | As directed by IQF | Required when shown on the plans in accordance with Item 585. |

5. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log or Non-Conformance Report Log.

6. Each test performed that is based on a quantity of material is considered “or fraction thereof” for calculating number of tests.

### Seal Coat

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

Table 2 - Seal Coat

| Material or Product | Test For | Test Number | Project Tests: Location or Time of Sampling | Project Tests: Frequency of Sampling8 | Remarks |
| --- | --- | --- | --- | --- | --- |
| Aggregate | Gradation7 | Tex-200-F, Part 1 | Stockpile (at source or at point of delivery) | 1 per 1,000 CY, per source | Rate may be reduced to 1 each 2,000 CY if the IQF approves a DB Contractor quality control plan. Sample in accordance with Tex-221-F. |
| Aggregate | L.A. Abrasion7 | Tex-410-A | Stockpile | 1 per source | Verify the published value of the source, as listed on the current Bituminous Rated Source Quality Catalog (BRSQC), meets the project Specifications. If not, sample 1 per 20,000 CY in accordance with Tex-221-F and submit to MTD for testing before use. |
| Aggregate | Magnesium Soundness7 | Tex-411-A | Stockpile | 1 per source | Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample 1 per 20,000 CY in accordance with Tex-221-F and submit to MTD for testing before use. |
| Aggregate | Surface Aggregate Classification7 | Tex-612-J, Tex-411-A | Stockpile | 1 per source | Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample 1 per 20,000 CY in accordance with Tex-221-F and submit to MTD for testing before use. |
| Aggregate | Pressure Slake7 | Tex-431-A | Stockpile | 1 per source | Required only for lightweight aggregate. Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample 1 per 20,000 CY in accordance with Tex-221-F and submit to MTD for testing before use. |
| Aggregate | Freeze Thaw7 | Tex-432-A | Stockpile | 1 per source | Required only for lightweight aggregate. Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample 1 per 20,000 CY in accordance with Tex-221-F and submit to MTD for testing before use. |
| Aggregate | Unit Weight | Tex-404-A | Stockpile | 1 per source | Required only for lightweight aggregate. Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample 1 per 20,000 CY in accordance with Tex-221-F and submit to MTD for testing before use. |
| Aggregate | 24-hour Water Absorption7 | Tex-433-A | Stockpile | 1 per source | Required only for lightweight aggregate. Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample 1 per 20,000 CY in accordance with Tex-221-F and submit to MTD for testing before use. |
| Aggregate | Crushed Face Count | Tex-460-A, Part 1 | Stockpile | 1 per 20,000 CY | Only required for crushed gravel. Sample in accordance with Tex-221-F. |
| Aggregate | Deleterious Material7 | Tex-217-F, Part 1 | Stockpile | 1 per 10,000 CY | Not required for lightweight aggregate. Sample in accordance with Tex-221-F. |
| Aggregate | Decantation7 | Tex-406-A | Stockpile | 1 per 10,000 CY | Sample in accordance with Tex-221-F. |
| Aggregate | Flakiness Index | Tex-224-F | Stockpile | 1 per source, or higher frequency as directed by the IQF | Sample in accordance with Tex-221-F. |
| Precoated Aggregate | Asphalt Content | Tex-236-F | Stockpile | 1 per source, per type (frequency as directed by the IQF when a target value is specified) | Sample in accordance with Tex-221-F. |
| Asphalt Binder | Compliance with Item 300 | N/A | Distributor Tested and preapproved by MTD. Take project samples when designated by the IQF. | 1 per grade, per source | Store and test in accordance with Item 316. Sample asphalt binder in accordance with Tex-500-C. Verify that the binder is from MTD’s preapproved source when it arrives at the project, and that the lab number on the shipping ticket is within the valid dates shown in the MTD QM test report. Binder should arrive at the project preapproved. |

7. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log or Non-Conformance Report Log.

8. Each test performed that is based on a quantity of material is considered “or fraction thereof” for calculating number of tests.

### Hydraulic Cement Concrete – Structural (Classes: C, F, H, S, CO, K, LMC, or SS)

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

Table 3 - Hydraulic Cement Concrete - Structural (Classes: C, F, H, S, CO, K, LMC, or SS).

| Material or Product | Test For | Test Number | Project Tests: Location or Time of Sampling | Project Tests: Frequency of Sampling | Remarks |
| --- | --- | --- | --- | --- | --- |
| Mineral Aggregate – Coarse Aggregate | Decantation | Tex-406-A, Part 1 | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. Part 1 testing frequency shall be kept at each 20,000 CY regardless of whether Part 3 is performed. |
| Mineral Aggregate – Coarse Aggregate | Decantation | Tex-406-A, Part 3 | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Perform Tex-406-A, Part 3, to increase the loss by decantation limit per the Specification. Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Coarse Aggregate | Sieve Analysis9 | Tex-401-A | From stockpile at concrete plant | Each 1,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. Test combined aggregate when used. |
| Mineral Aggregate – Coarse Aggregate | Deleterious Material | Tex-413-A | From stockpile at concrete plant | 1 per source and as necessary for control | Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Coarse Aggregate | Los Angeles Abrasion9 | Tex-410-A | From stockpile at concrete plant | Each 20,000 CY | Verify the value of the source, as listed on the current Concrete Rated Source Quality Catalog (CRSQC), meets the project Specifications. If not, sample and submit to MTD for testing before use in accordance with Tex-499-A. Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Coarse Aggregate | 5-Cycle Magnesium Sulfate Soundness9 | Tex-411-A | From stockpile at concrete plant | Each 20,000 CY | Verify the value of the source, as listed on the current CRSQC, meets the project Specifications. If not, sample and submit to MTD for testing before use in accordance with Tex-499-A. Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Fine Aggregate | Sand Equivalent | Tex-203-F | From stockpile at concrete plant | 1 per source and as necessary for control | Sample in accordance with Tex-400-A. Test combined aggregate when used. |
| Mineral Aggregate – Fine Aggregate | Organic Impurities | Tex-408-A | From stockpile at concrete plant | 1 per source | Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Fine Aggregate | Sieve Analysis9 | Tex-401-A | From stockpile at concrete plant | Each 1,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Fine Aggregate | Fineness Modulus | Tex-402-A | From stockpile at concrete plant | 1 per source and as necessary for control | Sample in accordance with Tex-400-A. Test combined aggregate when used. Test to confirm material variability when strength values are in question. |
| Mineral Aggregate – Fine Aggregate | Deleterious Material | Tex-413-A | From stockpile at concrete plant | 1 per source and as necessary for control | Sample in accordance with Tex-400-A. Test to confirm material variability when strength values are in question. |
| Mineral Aggregate – Fine Aggregate | Acid Insoluble (AI) Residue or Micro-Deval Abrasion (See Remarks)9 | Tex-612-J Tex-461-A | From stockpile at concrete plant | 2, each source | Only for concrete subject to direct traffic. Verify the AI value of the source, as listed on the CRSQC, meets the project Specifications. If not, sample and submit to MTD for testing before use in accordance with Tex-499-A. Alternatively, when blending fine aggregates, verify the AI and Micro-Deval values of the sources, as listed on the CRSQC, meet the project Specifications. If not listed on the CRSQC, sample and perform Micro-Deval testing, and sample and submit AI samples to MTD for testing, before use. Sample in accordance with Tex-400-A. |
| Mix Design | Compliance with the Standard Specification | N/A | At source (if not approved) | All designs per class, per source | Verify whether cement, coal ash, slag cement, silica fume, natural pozzolan, and chemical admixture sources are listed on the MPLs. If not listed on the MPL, sample and submit to MTD for testing before use. Sample in accordance with Tex-300-D for cement, in accordance with Tex-733-I for coal ash and natural pozzolan, in accordance with ASTM C989 for slag cement, in accordance with ASTM C1240 for silica fume, and in accordance with ASTM C494 for chemical admixtures. Water testing is contracted by the concrete supplier (commercial lab report to be reviewed by TxDOT). |
| Joint Material | Compliance with DMS-6310 | N/A | Sampled at jobsite if not prequalified by MTD | 1 per batch or shipment | Verify the source is listed on the MPL for joint sealers. If not, sample in accordance with Tex-500-C and submit to MTD for testing before use. For Class 6 joint sealers with nominal width less than 1.625 in. and joint fillers, IQF’s acceptance will be based on the review of the manufacturer-provided test report and physical observation. |
| Curing Compound | Compliance with DMS-4650 | N/A | Sampled at jobsite; tested by MTD | When requested by MTD | Only products listed on the MPL for concrete curing compounds will be allowed. When sample is requested by MTD, sample in accordance with Tex-718-I and submit to MTD for testing before use. Ensure container has been agitated and mixed before sampling. |
| Evaporation Retardants | Compliance with DMS-4650 | N/A | N/A | N/A | Only products listed on the MPL for evaporation retardants will be allowed. |
| Reinforcing Steel | Compliance with the Standard Specifications and Special Provisions | As specified | N/A | N/A | Only materials from MTD-approved sources listed on the MPLs for reinforcing steel mills and seven-wire steel strand will be allowed. |
| Mechanical Couplers | Compliance with DMS-4510 | Tex-744-I | Sampled at jobsite; tested by MTD | 3 couplers per lot (500 couplers) for each type, model, bar size, and grade | Only materials from MTD-approved sources listed on the MPL for mechanical couplers will be allowed. Sample in accordance with Tex-743-I and submit to MTD for testing. |
| Latex | Compliance with DMS-4640 for Concrete Chemical Admixtures | N/A | N/A | N/A | Verify the latex is listed on the MPL for chemical admixtures. If not, sample in accordance with ASTM C494 and submit to MTD for testing before use. |
| Epoxy | Compliance with DMS-6100, unless otherwise specified | N/A | Sampled at jobsite if not preapproved by MTD | 1 per batch or shipment | Verify the source is listed on the MPL for epoxies and adhesives. If not, sample in accordance with Tex-734-I and submit to MTD for testing before use. |
| Concrete | Compressive Strength9 | Tex-418-A | At point of concrete placement | 4 cylinders for each 60 CY (or fraction thereof) of concrete per day, per source, per class, per mix design For bridge railing and traffic railing: Testing may be reduced to 4 cylinders for each 180 CY (or fraction thereof) of concrete per day, per source, per class, per mix design | Sampling must be in accordance with Tex-407-A. Making additional cylinders for 56-day testing should be considered when slow strength gain mixtures are being used, or when the approved mix design has a history of failing to meet design strength at 28 days. Test 2 cylinders at 7 days, and if the average value is below the design strength as defined in Item 421, Table 8: Test the remaining 2 cylinders at 28 days; or If mutually agreed by IQF and TxDOT, test the remaining 2 cylinders at 56 days if additional cylinders were not made. If the average value of the 2 cylinders tested at 7 days meets the minimum design strength listed in Item 421, Table 8, the 2 remaining cylinders need not be tested. If the average value of the 7- and 28-day cylinders is below the design strengths, and 56-day cylinders were made, test the remaining set at 56 days. |
| Concrete | Slump | Tex-415-A | At point of concrete placement | 1 test, per 4 strength specimens | Sample in accordance with Tex-407-A. Perform slump and temperature tests on the same load from which strength test specimens are made. Check temperature of every load for bridge slabs and mass concrete placements. DB Contractor’s required testing will be in accordance with Specification requirements for the appropriate Specification Item. |
| Concrete | Entrained Air9 | Tex-416-A or Tex-414-A | At point of concrete placement | 1 test, per 4 strength specimens | Sample in accordance with Tex-407-A. Perform entrained air test only when entrained air concrete is specified on the plans. DB Contractor’s required testing will be in accordance with Specification requirements for the appropriate Specification Item. |
| Concrete | Temperature of Concrete9 | Tex-422-A | At point of concrete placement | 1 test, per 4 strength specimens | Sample in accordance with Tex-407-A. Perform slump and temperature tests on the same load from which strength test specimens are made. Check temperature of every load for bridge slabs and mass concrete placements. DB Contractor’s required testing will be in accordance with Specification requirements for the appropriate Specification Item. |
| Concrete | Top Slab Thickness and Depth of Reinforcement (for Bridge Deck or Culvert) | Tex-423-A, Part 2 | At or behind screed. Perform depth checks during dry run and during concrete placement (bridge deck and direct traffic culverts). | 1 test (3 depth check locations) per span per bay | Do not take depth measurements over a beam or girder. |

9. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log.

### Hydraulic Cement Concrete – Non-Structural Concrete (Classes: A, B, or E)

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

Table 4 - Hydraulic Cement Concrete - Non-Structural Concrete (Classes: A, B, or E).

| Material or Product | Test For | Test Number | Project Tests: Location or Time of Sampling | Project Tests: Frequency of Sampling | Remarks |
| --- | --- | --- | --- | --- | --- |
| Concrete | Compressive Strength10 | Tex-418-A | At point of concrete placement | 2 cylinders for each 180 CY (or fraction thereof) of concrete per day, per source, per class, per mix design | Strength will be determined by 7-day specimens. Sample in accordance with Tex-407-A. |
| Mix Design | Compliance with the Standard Specification | N/A | At source if not approved | All designs per class of concrete, per source | Verify whether cement, coal ash, slag cement, silica fume, natural pozzolans, and chemical admixture sources are listed on the MPLs. If not listed on the MPL, sample and submit to MTD for testing before use. Sample in accordance with Tex-300-D for cement, in accordance with Tex-733-I for coal ash and natural pozzolan, in accordance with ASTM C989 for slag cement, in accordance with ASTM C1240 for silica fume, and in accordance with ASTM C494 for chemical admixtures. Water testing is contracted by the concrete supplier (commercial lab report to be reviewed by TxDOT). |

10. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log or Non-Conformance Report Log.

### Grout (Various Applications)

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

Table 5 - Grout (Various Applications).

| Material or Product | Test For | Test Number | Project Tests: Location or Time of Sampling | Project Tests: Frequency of Sampling | Remarks |
| --- | --- | --- | --- | --- | --- |
| Rock/Soil Nail Anchors – Mix Design | Compliance with Standard Specification Item 410 and Item 411 | N/A | Before grout use in wall anchors | Review/approve each mix design | Verify whether cement, coal ash, slag cement, silica fume, natural pozzolans, and chemical admixture sources are listed on the MPLs. If not, sample and submit to MTD for testing before use. Water testing is contracted by supplier (commercial lab report to be reviewed by TxDOT). Sample in accordance with: Tex-300-D for cement, in accordance with Tex-733-I for coal ash and natural pozzolan, in accordance with ASTM C 989 for slag cement, and in accordance with ASTM C 1240 for silica fume. |
| Rock/Soil Nail Anchors – Approved Batch Plant Produced | Compressive Strength11 | Cylinders: Tex-418-A or Cubes: Tex-442-A | At point of placement | 1 test per 180 CY, per mix design12 | Sample in accordance with Tex-442-A or Tex-447-A. Strength will be determined by 7-day specimens. Cube strength based on average of 3 specimens (2-in. cubes). Cylinder strength based on average of 2 specimens (3"×6" cylinders). |
| Rock/Soil Nail Anchors – On-site Mixer Produced | Compressive Strength11 | Cylinders: Tex-418-A or Cubes: Tex-442-A | At point of placement | 1 test per 3,000 lb. of product12 | Sample in accordance with Tex-442-A or Tex-447-A. Strength will be determined by 7-day specimens. Cube strength based on average of 3 specimens (2-in. cubes). Cylinder strength based on average of 2 specimens (3"×6" cylinders). |
| Miscellaneous Applications – On-site Mixer Produced | Compressive Strength11 | Cylinders: Tex-418-A or Cubes: Tex-442-A (DMS-4675) | At point of placement | 1 test per day, per product12 | Sample in accordance with Tex-442-A or Tex-447-A. Strength will be determined by 7-day specimens. Cube strength based on average of 3 specimens (2-in. cubes). Cylinder strength based on average of 2 specimens (3"×6" cylinders). |
| Post-Tensioning – On-site Mixer Produced | Compressive Strength11 | Cylinders: Tex-418-A (DMS-4670) | At point of placement | 1 test per day, per product12 | Sample in accordance with Tex-447-A. Compressive strength is based on average of 2 specimens (3"×6" cylinders). Test 2 cylinders at 7 days, and if the average value is below the design strength as defined in the Specification, then test the remaining 2 cylinders at 28 days. |

11. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log or Non-Conformance Report Log.

12. First compressive strength specimens of any new structure shall be sampled during grout production for initial placement.

### Hydraulic Cement Concrete Pavement (Classes: P or HES)

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

Table 6 - Hydraulic Cement Concrete Pavement (Classes: P or HES).

| Material or Product | Test For | Test Number | Project Tests: Location or Time of Sampling | Project Tests: Frequency of Sampling14 | Remarks |
| --- | --- | --- | --- | --- | --- |
| Mineral Aggregate – Coarse Aggregate | Decantation | Tex-406-A, Part 1 | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. Part 1 testing frequency shall be kept at each 20,000 CY regardless of whether Part 3 is performed. |
| Mineral Aggregate – Coarse Aggregate | Decantation | Tex-406-A, Part 3 | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Perform Tex-406-A, Part 3, to increase the loss by decantation limit per the Specification. Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Coarse Aggregate | Sieve Analysis13 | Tex-401-A | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. Test combined aggregate when used. When producing optimized aggregate gradation (OAG) concrete, test every 10,000 CY of concrete in accordance with Tex-470-A. |
| Mineral Aggregate – Coarse Aggregate | Deleterious Materials | Tex-413-A | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Coarse Aggregate | L.A. Abrasion13 | Tex-410-A | From stockpile at concrete plant | 1, each source | Verify the value of the source, as listed on the current CRSQC, meets the project Specifications. If not, sample and submit to MTD for testing before use in accordance with Tex-499-A. Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Coarse Aggregate | 5-Cycle Magnesium Sulfate Soundness13 | Tex-411-A | From stockpile at concrete plant | 1, each source | Verify the value of the source, as listed on the current CRSQC, meets the project Specifications. If not, sample and submit to MTD for testing before use in accordance with Tex-499-A. Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Fine Aggregate | Sand Equivalent | Tex-203-F | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. Test combined aggregate when used. |
| Mineral Aggregate – Fine Aggregate | Organic Impurities | Tex-408-A | From stockpile at concrete plant | 1 per source | Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Fine Aggregate | Sieve Analysis13 | Tex-401-A | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. Test combined aggregate when used. When producing OAG concrete, test every 10,000 CY of concrete in accordance with Tex-470-A. |
| Mineral Aggregate – Fine Aggregate | Fineness Modulus | Tex-402-A | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. Test combined aggregate when used. When producing OAG concrete, test every 10,000 CY of concrete in accordance with Tex-470-A. |
| Mineral Aggregate – Fine Aggregate | Deleterious Material | Tex-413-A | From stockpile at concrete plant | Each 20,000 CY of concrete (each source) | Sample in accordance with Tex-400-A. |
| Mineral Aggregate – Fine Aggregate | Acid Insoluble (AI) Residue or Micro-Deval Abrasion (See Remarks)13 | Tex-612-J Tex-461-A | From stockpile at concrete plant | 1 per source | Verify the AI value of the source, as listed on the CRSQC, meets the project Specifications. If not, sample and submit to MTD for testing before use in accordance with Tex-499-A. Alternatively, when blending fine aggregates, verity the AI and Micro-Deval values of the sources, as listed on the CRSQC, meet the project Specifications. If not listed on the CRSQC, sample and perform Micro-Deval testing, and sample and submit AI samples to MTD for testing, before use. Sample in accordance with Tex-400-A. |
| Mix Design | Compliance with the Standard Specification | N/A | At source, if not approved | All designs, per class, per source | Verify whether cement, coal ash, slag cement, silica fume, natural pozzolan, and admixture sources are listed on the MPLs. If not listed on the MPL, sample and submit to MTD for testing before use. Sample in accordance with Tex-300-D for cement, in accordance with Tex-733-I for coal ash and natural pozzolan, in accordance with ASTM C989 for slag cement, in accordance with ASTM C1240 for silica fume, and in accordance with ASTM C494 for chemical admixtures. Water testing is contracted by the concrete supplier (commercial lab report to be reviewed by TxDOT). |
| Joint Material | Compliance with DMS-6310 | N/A | Sampled at jobsite if not prequalified by MTD. | 1 per batch or shipment | Verify the source is listed on the MPL for joint sealers. If not, sample in accordance with Tex-500-C and submit to MTD for testing before to use. For Class 6 joint sealers with nominal width <1.625 in. and joint fillers, IQF’s acceptance will be based on the review of the manufacturer-provided test report and physical observation. |
| Curing Compound | Compliance with DMS-4650 | N/A | Sampled at jobsite; tested by MTD. See remarks. | When requested by MTD | Only products listed on the MPL for concrete curing compounds will be allowed. Sample in accordance with Tex-718-I, when requested, and submit to MTD for testing. Ensure container has been agitated and mixed before sampling. |
| Evaporation Retardants | Compliance with DMS-4650 | N/A | N/A | N/A | Only products listed on the MPL for evaporation retardants will be allowed. |
| Reinforcing Steel | Compliance with the Standard Specifications and Special Provisions | As Specified | N/A | N/A | Only materials from MTD-approved sources listed on the MPL for reinforcing steel mills and seven-wire steel strand will be accepted. |
| Multiple Piece Tie Bars | Compliance with DMS-4515 | Tex-712-I | Sampled at jobsite; tested by MTD. See remarks. | 1 set (10 tie bars per sample set), for each type, model, bar size, and grade | Only materials from MTD-approved sources listed on the MPL for multiple piece tie bars for concrete pavements will be allowed. Sample in accordance with Tex-711-I. |
| Epoxy | Compliance with DMS-6100 | N/A | Sampled at jobsite, if not preapproved by MTD | 1 batch per shipment | Verify the source is listed on the MPL for epoxies and adhesives. If not, sample in accordance with Tex-734-I and submit to MTD for testing before use. |
| Concrete | Strength13, 14 | Tex-418-A | At point of concrete placement | 4 specimens for each 3,000 square yard (SY) of concrete per day or fraction thereof (per source, per class, per mix design) | Sample in accordance with Tex-407-A. Test 2 specimens at 7 days. If Item 360 strength requirements are not met, test the additional 2 specimens at 28 days. Or test job control samples at any age if proven to meet the 28-day compressive strength, as correlated in accordance with Tex-427-A. |
| Concrete | Slump | Tex-415-A | At time and location when strength specimens are made | 1 test, each time strength specimens are cast | Sample in accordance with Tex-407-A. Slump is not required for slip-formed pavement. Perform slump and temperature tests on the same load from which the strength specimens are made. |
| Concrete | Entrained Air13 | Tex-416-A or Tex-414-A | At time and location when strength specimens are made | 1 test, each time strength specimens are cast | Sample in accordance with Tex-407-A. Slump is not required for slip-formed pavement. Perform entrained air test only when entrained air concrete is specified on the plans. |
| Concrete | Temperature | Tex-422-A | At time and location when strength specimens are made | 1 test, each time strength specimens are cast | Sample in accordance with Tex-407-A. Perform slump and temperature tests on the same load from which the strength specimens are made. |
| Concrete | Thickness | Tex-423-A, Part 1 | Center of paving machine | Every 500 ft. or fraction thereof | Methods other than Tex-423-A may be shown on the plans. |
| Concrete | Depth of Joint Saw Cut | Tex-423-A, Part 3 | Within 24 hr. after saw cutting or before joints are sealed (whichever is sooner) | Every 500 ft. or fraction thereof for all longitudinal contraction joints and 10% of transverse contraction joints in CPCD for each daily placement | None |
| Concrete | Pavement Texture | Tex-436-A | Final riding surface of travel lanes | 1 per day, per driving lane | Perform when carpet drag is the only surface texture required as shown on the plans. |
| Concrete | Ride Quality13 | Tex-1001-S surface test Type B | Full length of final riding surface of all travel lanes | Each travel lane of finished surface | Perform the quality assurance (QA) testing as described in TxDOT Standard Specification Section 585.3.2.2.2. Report results from surface test Type A when requested by TxDOT. |

13. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log or Non-Conformance Report Log.

14. Each test performed that is based on a quantity of material is considered “or fraction thereof” for calculating number of tests.

### Hot-Mix Asphalt Pavement (Items 341, 342, 344, 346, 347, and 348)

This is a guide for minimum sampling and testing. Testing frequency may need to be increased for high material variability or when test results approach Specification limits.

All testing as noted in Table 7 below may be waived for exempt production as defined by Specification.

Table 7 - Hot-Mix Asphalt Pavement (Items 341, 342, 344, 346, 347, and 348).

| Material or Product | Test For | Test Number | Project Tests: Location | Project Tests: Frequency of Sampling | Remarks |
| --- | --- | --- | --- | --- | --- |
| Coarse Aggregate | L.A. Abrasion15 | Tex-410-A | Stockpile16 | 1 per aggregate source | Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample in accordance with Tex-221-F and submit to MTD for testing before use in accordance with Tex-499-A. |
| Coarse Aggregate | Magnesium Sulfate Soundness15 | Tex-411-A | Stockpile16 | 1 per aggregate source | Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample in accordance with Tex-221-F and submit to MTD for testing before use in accordance with Tex-499-A. |
| Coarse Aggregate | Surface Aggregate Classification15 | Tex-499-A | Stockpile16 | 1 per aggregate source | Verify the published value of the source, as listed on the current BRSQC, meets the project Specifications. If not, sample in accordance with Tex-221-F and submit to MTD for testing before use in accordance with Tex-499-A. |
| Coarse Aggregate | Micro-Deval Abrasion | Tex-461-A | Stockpile16 | 1 per aggregate source | Not required when the rated source soundness magnesium loss is 15 or less as listed on the current published BRSQC. If testing is required, sample in accordance with Tex-221-F. |
| Fine Aggregate | Sand Equivalent | Tex-203-F | Stockpiles, hot bins, or feeder belts | 1 per aggregate source, per design | Does not apply to Item 342. Sample in accordance with Tex-221-F. The timing of when the test is performed is at the discretion of the IQF. |
| Asphalt Binder | Compliance with Item 30015 | N/A | Sampling port nearest to the storage tank | 1 per grade, per source | Test a minimum of 1 sample taken from the project. Sample binder at hot-mix plant in accordance with Tex-500-C. Verify that the binder is from a preapproved source when it arrives at the project, and that the lab number on the shipping ticket is within the valid dates shown in the MTD QM test report. Binder should arrive at the project preapproved. |
| Tack Coat | Compliance with Item 30015 | N/A | Distributor | 1 per grade, per source | Test a minimum of one sample taken from the project. Sample tack coat in accordance with Tex-500-C. Verify that the binder is from a preapproved source when it arrives at the project, and that the lab number on the shipping ticket is within the valid dates shown in the MTD QM test report. |
| Mix Design Verification | Compliance with applicable Specification | Tex-204-F | At source (if not approved) | Min 1 design per mix type and asphalt grade | Verify that aggregates, recycled asphalt pavement, mineral filler, asphalt binder, anti-stripping additives, and warm mix systems are on the MPL where applicable and that they meet project Specification requirements. Project sampling and testing may be conducted on individual materials as necessary for control. A new mix design verification will be required if there is a change in aggregate sources. |
| Complete Mixture | Asphalt Content (%)15 | Tex-236-F | Truck sample | 1 per sublot | Sample in accordance with Tex-222-F. Determine correction factors for ignition oven using Tex-236-F once every 12 mo. or more frequently as needed. When Tex-236-F does not yield reliable results, the IQF may use an alternative method for determining asphalt content, such as Tex-210-F. |
| Complete Mixture | Voids in Mineral Aggregates (VMA) | Tex-204-F | Truck sample | 1 per sublot | Sample in accordance with Tex-222-F. Does not apply to Item 342 and Item 348. |
| Complete Mixture | Gradation15 | Tex-200-F | Truck sample | 1 per sublot | Sample in accordance with Tex-222-F. Determine correction factors for ignition oven using Tex-236-F once every 12 mo. or more frequently as needed. |
| Complete Mixture | Moisture Susceptibility | Tex-530-C | Truck sample | 1 per lot or as directed by the IQF | When shown on the plans. Sample in accordance with Tex-222-F. |
| Complete Mixture | Indirect Tensile Strength–Dry | Tex-226-F | N/A | 1 per mix design (Lot 1) | Sample in accordance with Tex-222-F. Does not apply to Items 342, 346, 347, and 348. |
| Complete Mixture | Moisture Content | Tex-212-F, Part 2 | Truck sample | 1 per mix design | Sample in accordance with Tex-222-F. |
| Complete Mixture | Lab-Molded Density15 | Tex-207-F, Parts 1, 6, and 8 | Truck sample | 1 per sublot | Sample in accordance with Tex-222-F. DB Contractor’s required testing will be in accordance with Specification requirements for the appropriate Specification Item. |
| Complete Mixture | Theoretical Maximum Specific Gravity | Tex-227-F | Truck sample | 1 per sublot | Sample in accordance with Tex-222-F. DB Contractor’s required testing will be in accordance with Specification requirements for the appropriate Specification Item. |
| Complete Mixture | Drain Down Test15 | Tex-235-F | Truck sample | 1 per sublot | Sample in accordance with Tex-222-F. Not required for Item 341 and Item 344. For Item 347, only required during design. |
| Complete Mixture | Hamburg Wheel Test15 | Tex-242-F | Truck sample | 1 per mix design | Sample in accordance with Tex-222-F. Sample during production. Required for all mixes. For Item 342 and Item 348, this test is only required for PFC-F during trial batch. |
| Complete Mixture | Cantabro Loss15 | Tex-245-F | Truck sample | 1 per mix design | Sample in accordance with Tex-222-F. Sample during production. Does not apply to Items 341, 344, 346, and 347. |
| Complete Mixture | Overlay Test15 | Tex-248-F | Truck sample | 1 per mix design | Sample in accordance with Tex-222-F. Sample during production. Only required for Item 346 and Item 347. |
| Roadway | In-Place Air Voids15 | Tex-207-F, Parts 1, 3, and 6 | Roadway | 2 cores per sublot | Two cores taken per sublot and averaged. Sample in accordance with Tex-222-F. Does not apply to Items 342, 347, and 348. |
| Roadway | Segregation Profile15 | Tex-207-F, Part 7 | Roadway | 1 per sublot | Not required when DB Contractor uses thermal imaging system. Does not apply to Items 342, 347, and 348. |
| Roadway | Joint Density15 | Tex-207-F, Part 8 | Roadway | 1 per sublot | Does not apply to Items 342, 347, and 348. |
| Roadway | Thermal Profile15 | Tex-244-F | Immediately behind paver | 1 per sublot | Not required when DB Contractor uses thermal imaging system. |
| Roadway | Ride Quality Test Type B15 | Tex-1001-S | Full length of final riding surface of all travel lanes | Each travel lane of finished surface | Perform the QA testing as described in TxDOT Standard Specification Section 585.3.2.2.2. Report results for surface test Type A when requested by TxDOT. |
| Roadway | Permeability15 | Tex-246-F | Roadway | 1 per sublot | Only applies to Items 342, 347, and 348. |
| Fabric Underseal | Compliance with DMS-6220 | N/A | Sampled, tested, and approved by MTD | N/A | Sampling must be in accordance with Tex-735-I. Verify the source is listed on the current MPL for silt fence, filter fabric, and fabric underseals. If not, sample and test before use in accordance with DMS-6220. |

15. When this project acceptance test fails but the product is accepted, document the reasons for acceptance on the Engineering Judgment Log or Non-Conformance Report Log.

16. Sampling may be performed at the plant, quarry, or both. Aggregate properties may be re-tested at any time during the project. These project tests may be used for one or more projects furnishing hot mix with the same aggregate source.